iClay 61H

Automotive Styling Clay | Technical Data Sheet

Product Description

iClay 61H is a high-hardness automotive styling clay formulated with synthetic waxes, oils and mineral fillers. It provides excellent surface definition, dimensional stability and machining performance for advanced styling models.

Applications

Automotive styling models
Transportation concept models
Industrial design prototypes
Appearance verification models

Key Features

• Fine texture and smooth surface finish
• Excellent carving and machining behavior
• High plasticity
• Suitable for CNC machining and precision refinement
• Stable long-term properties

Technical Data

| Property | Test Method | Specification |
| --- | --- | --- |
| Appearance | Visual inspection | Uniform color, smooth texture, no particles |
| Color | Visual inspection | Dark brown |
| Density (g/cm³) | GB 4472-84 | ≤1.1 |
| Hardness (23°C) | Shore C | 83-90 |
| Hardness (60°C) | Shore C | 0 |
| Recovered hardness (23°C/30min) | Shore C | 60-75 |
| Linear shrinkage (0-60°C) |  | <2.8×10⁻⁴ K⁻¹ |
| Shelf life |  | 2 years |

Hardness-Temperature Behavior

A cylindrical specimen was heated at 60°C and then cooled under 23°C room temperature conditions.

Processing Guidelines

Heat at approximately 55-60°C for 1-3 hours. Apply onto the model armature. After cooling, perform carving, trimming and surface refinement.

Packaging

Rod size: 270(±0.5) mm × Ø55 mm
Packing: 15 rods/carton

Storage

Store in a dry and cool place. Storage temperature: 10-25°C. Relative humidity: 0-50%.

Safety Precautions

Do not heat above 60°C. Avoid skin contact with hot material. Keep away from ignition sources.

Notes

Technical data are measured under specified conditions. Customers should conduct application testing before use.