iClay 61M
Automotive Styling Clay | Technical Data Sheet
Product Description
iClay 61M is a medium-hardness automotive styling clay formulated with synthetic waxes, oils and mineral fillers. It provides excellent formability, dimensional stability and extended working time for concept development and prototype styling applications.
Applications
Automotive styling models
Transportation concept models
Industrial design prototypes
Appearance verification models
Key Features
• Medium hardness grade
• Excellent workability after heating
• Extended working time for complex surfaces
• Easy carving with low tool resistance
• Low shrinkage and recyclable
Technical Data
	Property
	Test Method
	Specification

	Appearance
	Visual inspection
	Uniform color, smooth texture, no particles

	Color
	Visual inspection
	Yellow-brown

	Density (g/cm³)
	GB 4472-84
	≤1.1

	Hardness (23°C)
	Shore C
	75-85

	Hardness (60°C)
	Shore C
	0

	Recovered hardness (23°C/60min)
	Shore C
	60-75

	Linear shrinkage (0-60°C)
	
	≤2.8×10⁻⁴ K⁻¹

	Shelf life
	
	2 years


Hardness-Temperature Behavior
A cylindrical specimen was heated at 60°C and then cooled under 23°C room temperature conditions.
Processing Guidelines
Heat at approximately 55-60°C for 1-3 hours. Apply onto the model armature. After cooling, perform carving, trimming and surface refinement.
Packaging
Rod size: 270(±0.5) mm × Ø55 mm
Packing: 15 rods/carton
Storage
Store in a dry and cool place. Storage temperature: 10-25°C. Relative humidity: 0-50%.
Safety Precautions
Do not heat above 60°C. Avoid skin contact with hot material. Keep away from ignition sources.
Notes
Technical data are measured under specified conditions. Customers should conduct application testing before use.




